Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

Levante Labs Test Report b908

Pages 50 (including this one)

Authorized Signature

Test Approved for Release

Note: Hard copy available from Levante Labs. Send self addressed envelope to address above.

1

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

AIRSOFT BB AMMUNITION BALLISTIC TEST

1.  Introduction

2.  Aim

3.  Scope

4.  Preliminary Observations

5.  Velocity Tests

6.  Impact Tests

7.  Induced Expansion

8.  Human Target

9.  Conclusion

1. INTRODUCTION

We have been commissioned by our client to execute a study of 6mm ammunition used in the

sport/game  of  airsoft  (henceforth  bbs).  We  have  been  further  commissioned  to  execute

supplementary studies on new ammunition as soon as it is made available to the market. Our

client has asked us to limit the technical terms in this study so as to allow a person with no

prior experience in ballistics to understand the significance of the results. We have also been

asked to add our comments, observations and conclusions.

2. AIM

The  aim  of  this  study  is  to  execute  an  accurate  and  comparative  assessment  of  the

performance and safety of the bb ammunition when used in the game/sport of airsoft. To this

end  we  have  selected  and  acquired  a  wide  array  of  ammunition  by  both  manufacturer  and

weight class (FIG 1 in Annex).

3. SCOPE

3.1 This study was carried out under controlled environmental conditions in an indoor testing

range and laboratory. All results are expressed in SI units. Conversion to British Imperial Units

or American Units is to be executed using legally accepted conversion tables.

3.2  Ballistic  Clay  -  This  study  adopts  the  National  Institute  of  Justice  Standard  for  the

Ballistic Resistance of Body Armour (NIJ Standard - 0101.06) method of measuring back face

signature: a homogenous block of non hardening, oil-based modelling clay henceforth referred

to as ballistic clay.

3.3  Gun  Assembly  -  This  study  adopts  the  compressed  gas  gun  method  for  obtaining

consistent and repeatable muzzle velocities and impact velocities (henceforth gas gun). In this

configuration  peek  performance  was  attained  with  a  6.01mm  diameter  cold  hammer  forged

steel barrel, 50cm in length and coated with Teflon on the inside. This surface treatment on

the inside of the barrel is designed to drastically reduce the friction produced by the bb hitting

the walls of the barrel as it travels under the hop up and down to the muzzle. Gas pressure

and temperature was accurately monitored and maintained with each shot fired.

3.4  Methodology  -  The  bbs  were  fired  from  a  compressed  gas  gun,  with  controlled  air

pressure and temperatures, into ballistic clay, at impact targets and through speed traps. Each

bb was measured at muzzle velocity (V0) and impact velocities at a distance of 10m (V10),

20m (V20) and 30m (V30). Individual bb weight, bb diameter, depth of bb penetration into

ballistic clay, diameter of entry canal and velocity at impact were measured. A thinner sample

of  ballistic  clay  was  used  to  document  the  diameter  of  the  exit  canal  and  the  effects  of  bb

dynamics as they traveled through the ballistic clay.

2

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

3.5  Human  Target  -  The  bbs  were  fired  at  human  volunteer  targets  and  human  bone

simulators for visual recording and measurement of injury. The distance between the muzzle

of  the  gas  gun  and  the  human  target  and  bone  simulator  was  5m  (V5).  A  survey  of  the

volunteers was taken to decide the location of impact and the front thigh muscle was elected.

The muzzle was aimed at the front thigh muscle mass with a BDU placed tight against the skin

over the impact zone. A medical technician was called upon to supervise the test and to make

periodic visual inspections and observations of the individual wounds over a period of 4 days.

3.6  Cordura  on  Ballistic  Clay  -  The  bbs  were  fired  at  cordura  material  that  was  placed

against a block of ballistic clay. The distance between the muzzle and this target was V10. The

purpose of this test was to document the damage to the cordura and depth of the indentation

in the ballistic clay (Back Face Signature - BFS) measured by calculating the total area of the

indentation.

3.7 Cordura on Aluminum - The bbs were fired at cordura material that was placed against

an aluminum plate (type 6061 3mm thick). The distance between the muzzle and this target

was V10. The purpose of this test is to simulate and document the damage to cordura material

when a bb strikes a pouch loaded with standard airsoft rifle magazines.

3.8 BDU on Ballistic Clay - The bbs were fired at BDU material taken from the rear area of

Tru Spec BDU jacket made of poly-cotton (65%, 35%) rip-stop placed tight against a block of

ballistic clay. The purpose of this test is to document the effects of the impacts on the BDU and

the extent of the indentations (BFS) caused by the impacts on the ballistic clay.

3.9 Induced Expansion - The bbs were fired at a target with a 0.058mm sheet of cardboard

placed  against  a  block  of  ballistic  clay.  A  thin  block  of  clay  was  used  to  allow  the  bbs  to

completely traverse it and cause an exit hole on the reverse side. The purpose of this test is to

examine the dynamics of the impacts involved.

3.10  Face  Mask  -  The  bbs  were  fired  at  a  JT  style  mask.  This  system  provides  full  face

protection, a 280° optical visor fitted to a goggle support that affords a complete seal around

the eye area. This system provides protection against bbs fired from all directions and angles

and was deemed safe for the scope of this study.

3.11 Accuracy - Accurately quantifying V0, V10, V20, V30 is crucial to determine the effects

of  the  bbs  on  humans  and  on  property.  Ballistic  clay  was  used  in  various  instances  as  a

velocimeter. Calibration was achieved by correlating each bb's V0, V10, V20, V30 generated by

the compressed gas gun and measured with ballistic sensors, to the bb's depth of penetration

into the ballistic clay (BFS). Excellent repeatability was achieved. Calibration test was executed

by  loading  the  bb  into  the  gas  gun,  pressurizing  the  accumulator  and  firing  the  gun.  This

method   allows   accurate   measurements   and   provides   physical   evidence   which   can   be

photographed and compared for later study or for reference purposes (FIG A, B in Annex).

3.12 Talyrond and Mitutoyo metrology systems are used to measure the size, sphericity and

density of the bbs. Ballistic data measured with Oehler Research Inc instruments and in house

impact target systems.

3

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

4. PRELIMINARY OBSERVATIONS

Density

4.1 During the initial testing of the bbs it was confirmed that a very high percentage presented

considerable inconsistencies in material density within each of the bbs themselves. This was

documented and recorded into a chart shown in FIG 2 in Annex.

4.2 By measuring and analyzing different areas of the same bb a different density result was

recorded.  This  data  indicates  that  most  of  the  bbs  tested  are  therefore  to  be  considered

inhomogeneous  spherical  objects  with  asymmetric  densities.  This  conclusion  has  profound

negative consequences on the ballistic performance of this type of ammunition.

4.3 The most common problem of plastic and bio degradable bbs is the presence of small to

very  large  air  bubbles  and  the  extent  to  which  the  ingredients  are  properly  mixed.  These

inconsistencies  were  amplified  within  each  of  the  manufacturer's  bb  weight  class  and  within

each specific lot so that no 2 bbs were found with similar densities.

4.4 The root cause of inconsistent density in injection moulded plastics and bio-resins are as

follows:

4.4.1  manufacturing  process,  quality  control,  quality  of  plastic  resin,  quality  of

biodegradable resin, the mixing of ingredients;

4.4.2  The  limitations  imposed  by  the  plastic  or  bio-plastic  materials  themselves.

Perfectly uniform densities are difficult to achieve with plastics or biodegradable resins

relative to other materials. It is for this reason that good results are possible only if

great effort is placed in the manufacturing process and in the choice and use of the

ingredients involved.

4.5 In order to achieve good ballistic performance, a bb projectile with an imparted back spin

depends heavily on the uniform distribution of weight within its structure. This weight in turn

depends upon the density of the material measured at any point within the spherical structure

of  the bb itself.  Even  a slight  difference in  density  from one point  of  the bb to another will

cause its trajectory to deviate from the point of aim (FIG 3 in Annex).

4.6 Uniform density is a difficult quality to achieve in plastic bbs. The manufacturing process

may cause inconsistencies within each bb, from bb to bb, from lot to lot of the same brand and

from  brand  to  brand.  Consistent  performance  and  good  ballistics  require  high  quality

manufacturing procedures and ingredients.

4.7 Our test data concludes that the BBBMAX is noticeably different in terms of performance

and  density  from  other  bbs  in  the  test  since  most  probably  this  bb  is  not  moulded  (the

manufacturer has not furnished any details in this regard).

4.8  Our tests and observations concluded that the Digicon 0.43g bbs, the Bioval bio bbs  and

some  of  the  bbs  of  Japanese  manufacture  have  better  results  in  measured  densities  and

performance when compared to other bbs in the test. This is due to a better manufacturing

process, a higher quality control and to a higher quality of the materials used.

Magnus Effect

4.9 The back spin or rotational torque, known as the magnus effect, causes bbs to respond in

potentially  negative ways while in flight. Bbs have elastic properties that will cause them to

4

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

deform when force is applied to their structure. This deformation is a function of the applied

force and the material that they are made of. Once this force is removed the bb should return

to its original form. In this study, the difference between the original form and that measured

after  the  force  is  removed  is  the  degree  to  which  the  bb  is  actually  elastic  (or  not).  The

magnus effect imparts centripetal and centrifugal forces on the bb that together cause it to

deform inward along its spin axis (from pole to pole) and outward along the circumference of

its  equator.  This  deformation  is  proportional  to  its  rpm  and  its  elasticity  and  when  taken

together with the actual distribution of weight within the bb itself may have negative effects on

the  ballistics  of  the  bb  as  it  travels  along  the  barrel  and  as  it  travels  along  its  intended

trajectory to the target (FIG 4, 5 in Annex).

Sphericity and Diameter

4.10 The next issue confronting the initial testing process was the inconsistency in measured

sphericity and diameter of the bb samples. These data are based on the comparison of a near

perfect axis of rotation with the unknown quality of the bbs. Each bb was repeatedly measured

along a different axis. A total of 1000 bbs were measured from each manufacturer and each

weight class.

4.11 Spherical and diameter inconsistencies (within each bb, from bb to bb, from lot to lot,

from brand to brand) contribute to flawed mechanical performance within the gun as the bb

moves from the magazine, to the hop up chamber and as it travels down the barrel. Also, the

lack  of  elasticity  (defined  here  as  the  capacity  of  the  bb  to  return  to  its  original  spherical

shape) common to softer bbs does not allow them to regain their original spherical shape as

they  undergo  various  types  of  forces  within  the  magazine,  in  the  hop  chamber  and  finally

below and around the hop up itself. Inconsistent sphericity and lack of elasticity helps explain

some of the more common malfunctions associated with airsoft guns in general. On the other

hand, bbs that are too hard will crack or break within these mechanisms causing damage to

the  airsoft  gun.  The  correct  compromise  between  hardness,  softness  and  elasticity  is  only

possible with high quality manufacturing, quality control and the choice of correct materials.

Sphericity, as defined in this study, reflects all these issues taken together and is simplified in

one diagram shown in Fig 6 in Annex.

4.12 Spherical and diameter inconsistencies degrade ballistic performance (with each bb, from

bb to bb, from lot to lot, from brand to brand) since the aerodynamics of the bb is affected

during flight. This difficulty is further magnified with the application of the hop up device since

this setting must be placed at relative constant to get consistent data and to hit the targets.

4.13 Sphericity is a notoriously difficult quality to achieve in plastic and bioplastic materials.

The process of removing mould marks, injection port sprues, injection port marks and other

surface  imperfections  may  cause  inconsistencies  in  sphericity  and  diameter  within  each  bb,

from bb to bb, from lot to lot and from brand to brand.

4.14 Our tests and observations conclude that the BBBMAX is the most consistent bb tested.

This  supports  our  view  that  most  probably  this  bb  is  not  moulded  and  therefore  the

manufacturing  process  adopts  a  more  accurate polishing  system.  The  manufacturer  has  not

provided details in this regard.

4.15  Our tests and observations concluded that the Digicon 0.43g bbs, the Bioval bio bbs and

some bbs of Japanese manufacture are noticeably different from other bbs in the test. Again,

this is propably due to better manufacturing process, higher quality control and higher quality

of material used.

5

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

5. Velocity V0, V10, V20, V30

V0 (FIG.7,8,9)

5.1 The Velocity at V0 in m/s was measured using a precision speed trap placed at the muzzle

of the gas gun and a block of ballistic clay placed behind the speed trap. This part of the study

examines the dynamics of the bb as it is accelerated down the barrel and is known as interior

ballistics.  In  this  phase,  the  bb's  acceleration  is  affected  by  5  forces  that  are  acting  on  its

forward motion and ultimately affecting the measured muzzle velocity: (1) the gas pressure

behind the bb; (2) the back spin or rotational torque (magnus effect) imparted on the bb by

the hop up mechanism; (3) the rpm of the back spin. This spin may also deform the bb to

some degree see 4.9 above; (4) the air resistance in front of the bb; (5) the friction of the bb

against the barrel. This force is not uniform since it depends on the condition of the barrel and

on the diameter, sphericity and smoothness of the bb.

5.2 The events that occur as the bb interfaces with the barrel and the forces described in 4.9

and 5.1 above are crucial to the trajectory of the bb when it leaves the barrel of the gun. An in

depth study of the interior ballistics of each bb is beyond the scope of this study and for this

reason we have chosen to set specific parameters by using the gas gun apparatus as described

in 3.3 above. Suffice it to say that the forces interacting with the bb in the barrel will inevitably

be dissimilar and inconsistent (from shot to shot) in a different set up from that described in

this study. Our test apparatus forms an ideal neutral test basis necessary to record accurate

measurements of the bb as it leaves the barrel. It is for this reason that gun tests and bb tests

outside an ideal parameter are to be regarded as highly suspect and wholly inaccurate.

5.3  The  results  of  V0  were  recorded  in  FIG.7,8,9  and  were  executed  at  3  different  power

settings of the gas gun. These settings are represented by the V0 of our control bbs in each of

the tables. All other bbs within each table were tested at the power settings of the control bbs

thus enabling an accurate comparison of each bb's performance relative to its competitor.

5.4 Interpreting the results of FIG 7,8,9. The higher the speed of the bb the more efficiently

the  bb  is  able  to  cope  with  the  forces  it  is  interacting  with  in  the  gas  gun  test  barrel.  The

results  represent  the  average  V0  in  m/s  of 1000  bbs  fired  for  each  brand  and weight (FIG

7,8,9 in Annex).

V10 (FIG 10,11,12)

5.5  As  the  bb  leaves  the  barrel  the  situation  changes  drastically.  The  propellant  pressure

behind the bb drops violently to the local atmospheric pressure. The gas gun ceases to be an

influencing factor in the bb's trajectory.

5.6 At this point Newton's laws of motion come into play and the science of external ballistics

is applied to understand the dynamics of the forces that act on the bb.

5.7 In this phase, the bb's trajectory is affected by the following forces: (1) Drag force, or the

force  acting  against  the  bb's  forward  motion.  (2)  the  rpm  of  the  back  spin;  (3)  the  elastic

deformation of the bb (see 4.9 above); (4) the bb's gyroscopic motion; (5) the V0 of the bb.

These  forces  taken  together  will  slow  the  bb  down  (negative  acceleration)  and  change  its

trajectory.

5.8 The results of V10 were recorded in FIG 10, 11, 12 . The initial V0 in m/s and the power

settings recorded earlier form the basis of the results recorded in the V10 tables. As explained

in 5.3 above, all the results help compare the performance of each bb against the control bbs

and against their competitors.

6

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

5.9  Interpreting  the  results  in  FIG  10,11,12.  The  higher  the  speed  of  the  bb  the  more

efficiently  the  bb  is  able  to  cope  with  the  forces  it  is  interacting  with  as  it  travels  along  its

trajectory. The results represent the average V10 in m/s of 1000 bbs fired for each brand and

weight (FIG 10,11,12 in Annex).

V20 and V30 (FIG 13 to 17)

5.10 The counterintuitive nature of external ballistics becomes very apparent in the results of

the bbs' performance out to V20 and V30.

5.11 Many of the bbs tested were unable to hit their intended targets in a consistent manner

and therefore results were unattainable. This is reflected in the V20 and V30 tables by a lack of

data. The main cause of this can be explained by the magnus and gyroscopic forces, influenced

by  the  inconsistent  sphericity  and  density  within  the  bbs,  changing  the  trajectory  in  a  very

noticeable manner (FIG 3,4,5 in Annex).

5.12  The  results  of  V20/V30  were  recorded  in  FIG  13  to  17.  The  initial  V0  is  m/s  and  the

power settings recorded earlier form the basis of the results recorded in the V20/V30 tables.

As explained in 5.3 above all the results help compare the performance of each bb against the

control bbs and against their competitors.

5.13  Interpreting  the  results  in  FIG  13  to  17.  The  higher  the  speed  of  the  bb  the  more

efficiently  the  bb  is  able  to  cope  with  the  forces  it  is  interacting  with  as  it  travels  along  its

trajectory. The results represent the average V20/V30 in m/s of 1000 bbs fired for each brand

and weight (FIG 13,14,15,16,17).

6. Impact Tests

6.1 The result of any impact between two objects depends on the force and time during which

the objects are in contact.

6.2 The time the two impacting objects remain in contact depends on the material properties

of the two objects.

6.3 The softer the objects the more time they will remain in contact.

6.4 With sufficient force the objects will either break or deform.

Observations and Comments

6.5 This section of testing is based on the laws of physics (described in 6.1, 6.2, 6.3 and 6.4)

above  to  determine  bb  impact  results  against  various  types  of  material  and  against  airsoft

players. As a preliminary test it was necessary to carry out impact tests of all the bbs involved

to  record  their  physical  properties.  In  general,  it  was  observed  that  the  BBBMAX  does  not

deform during impact and will not readily break while all other bbs will deform to some degree

and some will easily break. Deformation was permanent at elevated speeds for some softer

bbs.  Harder  plastic  or  bio  bbs  either  regained  much  of  their  original  form  or  shattered

catastrophically.

6.6  Testing  against  masks  and  mask  optics,  involved  firing  bbs  at  the  visor  assembly  and

mask  body.  NB  This  test  was  necessary  in  terms  of  the  scope  of  this  report  but  does  not

represent  a  homologation  test  of  the  masks  involved.  For  more  precise  information  please

refer  to  the  manufacturers  safety  warnings  and  their  declared  level  of  homologation.

Nevertheless, it was observed that all masks adopting a wire mesh visor assembly instead

7

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

of a transparent plastic or polycarbonate optical visor assembly caused the bbs to shatter or

were  penetrated.  This  catastrophic  failure  can  cause  extreme  and/or  permanent  eye  injury.

The wire mesh masks were deemed too dangerous for further testing and removed from the

test location.

Cordura against hard surface at V0, V10, V20, V30 speed set 130/170

V0 130/170

6.7  The  first  test  involved  setting  up  a  target  with  one  layer  of  cordura  denier  1000  tight

against a hard aluminium 6061 plate 3mm thick. The purpose of this test is to document the

extreme  dynamics  and  resulting  damage  to  cordura  material  when  a  bb  strikes  the  target

assembly.

6.8 The distance between the muzzle and this target was V0 (point blank) and the bbs were

fired at the speed settings described in 5.3 above. This test simulates a pouch loaded with an

airsoft  rifle  magazine  on  a  load  bearing  vest  of  a  type  normally  used  by  players.  This  test

represents  a  worst  case  scenario  since  (1)  most  magazines  have  an  irregular  surface  area

therefore not all of the area would  be exposed to this type of impact; (2) point blank impacts

are  rare.  Nevertheless,  an  extreme  case  was  necessary  to  form  a  database  of  control  data

against which future tests (below) could be compared to.

6.9 In general, due to their elastic properties, plastic and bio bbs tend to expand on impact

and  will  cause  a  wider  area  of  damage  to  the  fibers  than  harder  bbs.  Harder  bbs  will  not

deform  and  expand  and  will  cause  a  more  focused  and  much  smaller  area  of  damage.  The

results of the test were photographically recorded and documented.

6.10 Plastic and bio bb impacts on the cordura material are characterized by individual cordura

fiber breakage. Three types of damage were observed: (1) in some cases the heat produced

by  the  impact  will  cause  individual  cordura  fibers  to  melt  and  to  bind  with  the  surrounding

fibers limiting further damage; (2) in other instances the cordura did not melt and may result

in further damage as the individual damaged cordura fibers come unraveled from the weave.

With  time  and  heavy  usage  this  result  may  cause  the  damaged  area  to  expand  since  the

mechanical  resistance  of  the  cordura  fabric  is  compromised.  (3)  in  many  instances  a

combination of melted fibers and broken fibers were observed. In this case, the structure of

the cordura fabric may be compromised and cause further damage with time and heavy usage.

6.11 Harder bbs, such as the BBBMAX, tend to cause much smaller damage areas since they

will not deform and expand on impact. The heat produced by the impact will cause individual

cordura fibers to melt and to bind with the surrounding fibers. The small nature of this damage

and the fact that the damaged fibers are fastened (melted) to the surrounding structure will

severely limit further damage with time and heavy usage.

V10 at 130/170

6.12 The second test involved setting up a target with one layer of cordura denier 1000 tight

against a hard aluminium 6061 plate 3mm thick. The purpose of this test is to document the

extreme  dynamics  and  resulting  damage  to  cordura  material  when  a  bb  strikes  the  target

assembly.

6.13 The distance between the muzzle and this target was V10 (10m) and the bbs were fired

at the speed settings described in 5.3 above. This test simulates a pouch loaded with an airsoft

rifle magazine on a load bearing vest of a type normally used by players. As in 6.8 above, this

test  represents  a  worst  case  scenario  since  most  magazines  have  an  irregular  surface  area

8

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

therefore not all of the area would  be exposed to this type of impact. Nevertheless, impacts at

this distance are more likely to occur.

6.14 Plastic and bio bbs generally tend to deform and expand on impact to a lesser degree

than described in 6.9 above since the force of impact is reduced. Nevertheless, they will cause

a wider area of damage to the fibers relative to harder bbs. Harder bbs will not deform and

expand and will cause a more focused and much smaller area of damage. The results of the

test were photographically recorded and documented.

6.15 At this greater distance it was observed that Plastic and bio bb impacts on the cordura

material  are  characterized  by  individual  cordura  fiber  breakage  but  too  a  lesser  degree.  A

repetition of the three types of damage observed in 6.10 above were recorded.

6.16 At this greater distance the damage caused by harder bbs, such as the BBBMAX, tend to

cause an even smaller damage area and to a lesser degree than those described in 6.10, 6.11,

6.14 above. The is due mainly to the fact that hard bbs will not deform and expand on impact

(FIG C, D).

V20/V30 at 130/170

6.17 At these medium and extreme distances exactly the same target assembly as described

in 6.7 and 6.12 was used though with roughly double the size since it was difficult for many

bbs to actually hit the target.

6.18 This test represents the most likely distance of engagement in most airsoft games. Due

to the irregular surface area of most airsoft magazines not all of the area would  be exposed to

this type of impact.

6.19 At these extreme distances the results were a repetition of those recorded in the sections

6.7 to 6.18 above though to a degree proportional to the greater distance and therefore much

smaller forces were involved.

6.20 At these distances recorded damage was fundamentally different than that of previous

tests. Statistically, the force transferred to the cordura was not enough to cause any damage

to  the  cordura  structure.  Nevertheless  some  damage  was  recorded  with  the  following

characteristics: Plastic and bio bbs will still deform and expand but due to the reduced force

any  resulting  damage  was  limited  to  broken  fibers  with  no  melting;  heavy  bbs  still  caused

melting and breakage of fibers.

Cordura against soft surface at V0, V10, V20, V30 speed set 170

6.21 This test involved setting up a target with one layer of cordura denier 1000 placed tight

against  a  block  of  ballistic  clay.  The  purpose  of  this  test  is  to  document  the  effects  of  the

impacts on the cordura and the extent of the indentations caused by the impacts on the clay.

6.22 The target was placed at various distances (V0, V10, V20, V30) and the bbs were fired at

the 170 speed settings described in 5.3 above. This test simulates the impact of a bb on a soft

back drop such as human skin.

V0 at 170

6.23 No penetrations of the cordura material were observed by any bb.

6.24  Damage  to  the  cordura  was  very  limited  with  some  very  limited  fiber  damage  but

absolutely no holes.

9

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

6.25 By examining and measuring the bbs after the impacts it was observed that all plastic

and bio bbs and the digicon expanded and deformed on impact as they decelerated into the

ballistic clay. Hard bbs (bbbmax) did not deform or expand as they decelerated into the clay.

No bb breakage was recorded during testing.

6.26 By observing the indentations caused by the bbs impacting into the ballistic clay we were

able  to  estimate  the  total  energy  transfer  of  the  impacting  bbs.  The  remaining  energy  was

expended by the bbs rebounding off the targets.

6.27 Digicon 0.43g - the measured impact area caused by the digicon bbs was 12 times larger

than the measured area of the bb. This result is a function of the bbs weight, the amount of

deformation and expansion upon impact.

6.28 Plastic & bio 0.28g/0.30g - the average measured impact area caused by these heavy

bbs was 11 times larger than the measured area of the bb. This result is a function of the bbs

weight, the amount of deformation and expansion upon on impact.

6.29 Plastic & Bio 0.23g/0.25g - the average measured impact area caused by these medium

bbs was 10.5 times larger than the measured area of the bb. This result is a function of the

bbs weight, the amount of deformation and expansion upon impact.

6.30 BBBMAX - the average measured impact area caused by the BBBMAX was 7 times larger

than the measured area of the bb.

6.31 Plastic & bio 0.20g - the average measured impact area caused by the light bbs was 6

times larger than the measured area of the bb. This result is a function of the bbs weight, the

amount of deformation and expansion upon on impact.

6.32 Conclusion - in proportion to their weight and size, the energy transferred from the bb to

the target ballistic clay via the cordura is much greater with all plastic, bio and digicon bbs

than with the BBBMAX.

V10 at 170

6.33 No penetrations of the cordura material were observed by any bb.

6.34  Damage  to  the  cordura  was  very  limited  with  some  very  limited  fiber  damage  but

absolutely no holes.

6.35 By observing and measuring the bbs after the impacts it was observed that all plastic, bio

and the digicon expanded and deformed on impact as they decelerated into the ballistic clay.

Hard  bbs  (bbbmax)  did  not  deform  or  expand  as  they  decelerated  into  the  clay.  No  bb

breakage was recorded during testing.

6.36 By observing the indentations caused by the bbs impacting into the ballistic clay we were

able  to  estimate  the  total  energy  transfer  of  the  impacting  bbs.  The  remaining  energy  was

expended by the bbs rebounding off the targets.

6.37 Digicon 0.43g - the measured impact area caused by the digicon bbs was 8 times larger

than the measured area of the bb. This result is a function of the bbs weight, the amount of

deformation and expansion upon on impact.

10

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

6.38 Plastic & bio 0.28g/0.30g - the average measured impact area caused by the heavy bbs

was  7  times  larger  than  the  measured  area  of  the  bb.  This   result  is  a  function  of  the  bbs

weight, the amount of deformation and expansion upon on impact.

6.39 Plastic & bio 0.23g/0.25g - the average measured impact area caused by the medium

bbs was 6.5 times larger than the measured area of the bb. This result is a function of the bbs

weight, the amount of deformation and expansion upon on impact.

6.40 BBBMAX - the average measured impact area caused by the BBBMAX was 4 times larger

than the measured area of the bb.

6.41 Plastic & bio 0.20g - the average measured impact area caused by the light bbs was 3

times larger than the measured area of the bb. This result is a function of the bbs weight, the

amount of deformation and expansion upon on impact.

6.42 Conclusion - in proportion to their weight and size, the energy transferred from the bb to

the target clay via the cordura is much greater with all plastic, bio and digicon bbs than with

the BBBMAX (FIG E).

V20/V30 at 170

6.43 No damage or penetrations of the cordura material were observed.

6.44 Due to the small amount of energy retained in the bbs at V20 and V30 small and very

small indentations were observed in the ballistic clay relative to the results recorded in 6.21 to

6.42 above.

6.45  Digicon  -  At  V20  the  digicons  still  retained  enough  energy  to  cause  indentations  that

were larger than their size. At V30 indentations were either the same size or smaller than the

size of the bb.

6.46 Plastic & bio 0.28g/0.30g - At V20 the heavy bbs still retained enough energy to cause

indentations that were larger than their size. At V30 indentations were either the same size or

smaller than the size of the bb.

6.47 BBBMAX - At V20 the BBBMAX still retained enough energy to cause indentations that

were larger than their size. At V30 indentations were either the same size or smaller than the

size of the bb.

6.48 Plastic & bio 0.20g - At V20 not all the light bbs were able to hit the target. Those that

did caused indentations that were smaller than their size. Tests at V30 were suspended since

no bb was able to hit the target.

6.49 Conclusion - in proportion to their weight and size, the energy transferred from the bb to

the target clay via the cordura is much greater with all plastic, bio and digicon bbs than with

the BBBMAX.

BDU against soft surface at V10, V20, V30 speed set 170

6.50 This test involved setting up a target with one layer of olive drab material taken from the

rear  area  of  Tru  Spec  BDU  jacket  made  of  poly-cotton  (65%,  35%)  rip-stop  placed  tight

against  a  block  of  ballistic  clay.  The  purpose  of  this  test  is  to  document  the  effects  of  the

impacts on the BDU and the extent of the indentations caused by the impacts on the ballistic

clay.

11

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

6.51 The target was placed at various distances (V10, V20, V30) and the bbs were fired at the

170 speed settings described in 5.3 above. This test simulates a worst case scenario of the

impact of a bb on a soft back drop.

V10 at 170

6.52 The Digicon 0.43g bb penetrated the BDU. Non of the other bbs penetrated the BDU.

6.53 The Digicon 0.43g bb caused a hole in the BDU seriously damaging the fabric. Non of the

other bbs caused any damage to the BDU material except small indentations that were fixed

by placing some warm water on the material and flattening them out.

6.54 By observing and measuring the bbs after the impacts it was observed that all plastic, bio

and the digicon bbs expanded and deformed on impact as they decelerated into the ballistic

clay. Hard bbs (bbbmax) did not deform or expand as they decelerated into the clay. No bb

breakage was recorded during testing.

6.55 By observing the indentations caused by the bbs impacting into the ballistic clay we were

able  to  estimate  the  total  energy  transfer  of  the  impacting  bbs.  The  remaining  energy  was

expended  by  the  bbs  rebounding  off  the  targets.  The  Digicon  0.43g  bb  transferred  all  its

energy into the BDU material and into the ballistic clay.

6.56 Digicon 0.43g - this bb penetrated the BDU material and was found lodged 25mm into

the ballistic clay. The total measured impact area of the entry channel was 21 times the size of

the bb. This result is a function of the bbs weight, the amount of deformation and expansion

upon impact.

6.58 Plastic & bio 0.28g/0.30g - the average measured impact area caused by the heavy bbs

was 13 times larger than the measured area of the bb. This is result is a function of the bbs

weight, the amount of deformation and expansion upon impact.

6.58 Plastic & bio 0.23g/0.25g - the average measured impact area caused by the medium

bbs was 11 times larger than the measured area of the bb. This is result is a function of the

bbs weight, the amount of deformation and expansion upon impact.

6.59 BBBMAX - the average measured impact area caused by the BBBMAX was 7 times larger

than the measured area of the bb.

6.60 Plastic & bio 0.20g - the average measured impact area caused by the light bbs was 8

times larger than the measured area of the bb. This is result is a function of the bbs weight,

the amount of deformation and expansion upon impact.

6.61  Conclusion  -  the  impact  caused  by  the  bbs  in  the  cordura  are  a  little  smaller  when

compared  to  the  results  above.  All  conditions  being  equal,  the  only  difference  between  the

cordura soft target tests (6.21 to 6.49) and the results above (6.50 to 6.60) is the nature of

the material placed between the bbs and the ballistic clay. Cordura is able to cause the bbs to

expand  more  than  poly-cotton  but  cordura  is  also  able  to  dissipate  the  bb's  impact  more

efficiently along its fibers than the poly-cotton in the BDU. In proportion to their weight and

size, the energy transferred from the bb to the target clay via the BDU is much greater with all

plastic, bio and digicon bbs than with the BBBMAX (PLACE FIG F, G, H).

V20/V30 at 170

6.62 No penetrations were observed.

12

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

6.63 No damage of any nature was observed.

6.64 The impacts observed at V20 caused by the plastic and the digicon bbs into the ballistic

clay  were  smaller  than  at  V10.  Hard  bbs  (bbbmax)  did  not  deform  or  expand  as  they

decelerated  into  the  clay  and  caused  even  smaller  indentations  at  V20  and  V30.  No  bb

breakage was recorded during testing.

6.65 By observing the indentations caused by the bbs impacting into the ballistic clay we were

able  to  estimate  the  total  energy  transfer  of  the  impacting  bbs.  The  remaining  energy  was

expended by the bbs rebounding off the targets.

6.66 Digicon 0.43g - the average measured impact area caused by the heavy plastic bbs was

slightly larger than the measured area of the bb.

6.67  Plastic  &  bio  0.28g/0.30g  -  the  average  measured  impact  area  caused  by  the  heavy

plastic bbs was slightly larger than the measured area of the bb.

6.68 Plastic & bio 0.23g/0.25g - the average measured impact area caused by the medium

plastic bbs was smaller than the measured area of the bb.

6.69 BBBMAX - the average measured impact area caused by the BBBMAX was smaller than

the measured area of the bb.

6.70 Plastic & bio 0.20g - At V20 not all the light bbs were able to hit the target. Those that

did caused indentations that were smaller than their size. Tests at V30 were suspended since

no bb was able to hit the target.

6.71 Conclusion - at V20 and V30 the recorded indentations were negligible but slightly larger

than  those  recorded  in  the  cordura     tests  above  (6.21  to  6.49).  This  is  due  to  the

characteristics of the cordura material that is able to better dissipate the impact energy along

its fibers at the V20 and V30 distances. As in previous test, and in proportion to their weight

and size, the energy transferred from the bb to the target clay via the BDU is much greater

with all plastic, Bio and digicon bbs than with the BBBMAX.

Full Face Protective Systems

6.72 NB This test was necessary in terms of the scope of this report but does not represent a

homologation  test  of  the  face  and  eye  protective  systems  involved.  For  more  precise

information  please  refer  to  the  manufacturers  safety  warnings  and  their  declared  level  of

homologation. Furthermore, we do not recommend or condemn the use of any type of face

and eye protective systems. The purpose of this test is to study the possible types of damage

bb ammunition can cause on face and eye protection and to understand the dynamics of bb

ammunition against face and eye protective systems.

6.73 High velocity projectiles such as all bbs of any manufacturer used in the sport/game of

airsoft are potentially very dangerous and may cause severe eye and face injury and damage

to  teeth.  In  many  instances  damage  and  injury  may  be  permanent.  Always  wear  full  face

protection with fully sealed goggles using homologated optics (henceforth Mask) on the game

field  and  during  preparation  before  a  game.  Never  use  any  Masks  until  you  have  read,

understood  and  followed  all  instructions  and  safety  precautions/warnings  provided  by  the

manufacturer. Never remove the Mask while on the game field or during preparation.

6.74 The producers of Masks typically state the following precautions must be followed closely

(this is not an exhaustive list and other precautions may be stated by some manufacturers):

Any impact on the Mask optics may damage its structure. Always inspect the protective Mask

13

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

for small cracks each time before you play and replace it immediately if any cracks are found.

Always  replace  the  optics  every  time  they  are  shot  even  if  you  cannot  see  any  cracks  or

evidence of damage. This is because the structure of the optics may be compromised and fail

catastrophically  with  future  impacts.  Always  replace  the  optics  at  least  once  per  year,

beginning with the date of purchase. Atmospheric conditions will degrade the structure of the

optics with time. Always inspect the entire Mask that you are borrowing or renting using the

above criteria.

6.75  Chemicals,  heat,  sunlight,  fumes  and  other  products  and  atmospheric  conditions  may

degrade the structure of the Mask and optics and cause the system to fail when impacted by a

projectile. Read the owners manual and follow the instructions regarding storage and cleaning

very carefully.

6.76 In order to remain within the scope of this study, masks must provide a complete seal

around the eyes to prevent bb penetration when fired from multiple angles and directions. All

other systems were removed from the test area.

6.77  SPECIFICALLY:  it  was  observed  that  all  masks  adopting  a  wire  mesh  visor  assembly

instead of a transparent plastic or polycarbonate optical goggle visor assembly caused the bbs

to shatter or were penetrated. This catastrophic failure can cause extreme and/or permanent

eye injury. The wire mesh masks were deemed too dangerous for further testing and removed

from the test location.

6.78  SPECIFICALLY:  It  was  observed  that  sunglass  style  ballistic  protection  was  unable  to

prevent bbs from penetrating into the area behind the lenses when fired from multiple angles

and directions. Wrap around styles also failed. Many bbs impacting around this type of system

rebounded off the test supports and were found lodged behind the optics. The sunglass style

ballistic protection were deemed too dangerous and removed from the test area.

6.79 For the purposes of this test a JT style mask was used. This system provides full face

protection, a 280° optical visor fitted to a goggle support that affords a complete seal around

the eye area. This system provides protection against bbs fired from all directions and angles

and was deemed sufficiently safe for the scope of this study. Please see 6.72 to 6.78 above.

6.80 For the purposes of this study two possible types of full face protective system failures

are possible on the tested Mask (WARNING: other types of failure may be possible. Please read

the manufacturers full face protection level of homologation for more precise information and

see 6.72 to 6.78 above): (1) penetration of the mask and/or the optics and (2) spalling.

6.81  Penetration  of  the  mask  occurs  when  the  bb  impacts  with  sufficient  force  to  travel

through the protective material or protective optics. The bb will then continue to travel and

strike the wearer in the eyes or face. Collateral damage occurs when the bb causes shattering

of the protective Mask material or optics thereby increasing the degree of injury to the wearer.

This type of injury may cause permanent eye damage.

6.82  Spall  may  occur  when  a  bb  strikes  the  Mask  or  optical  protection  on  the  mask.  Upon

impact, flakes of material are broken off a Mask or optical body. When a projectile impacts a

hard surface but does not have enough energy to penetrate the surface, it will create a shock

wave that travels through the material and will break the material on the inside of the Mask or

optics. This broken material is known as spall and may have sufficient energy to travel across

the space between the Mask/optics and eyes/face and may cause injury to the eyes/face on

the inside of the Mask/optics.

6.83 The purpose of this test is to document the effects of the expansion and deformation of

the bbs caused by the impact against a full face mask protective system and against the optics

14

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

of the Mask. By observing the damage and the effects of the impacts more accurate evidence

can  be  recorded  of  the  dynamics  involved.  This  test  represents  a  real  world  worst  case

scenario.

6.84 This test involved setting up a JT nForcer full face mask fixed to a support as the target.

The type of supports used prevented the Mask and optics to flex or bend as a result of the bb

impacts.  A  block  of  ballistic  clay  was  placed  behind  the  target  set  up  to  record  any

penetrations or spall resulting from the impact.

6.85 All the bbs tested at V0 speed setting 170 (see 5.53 above) caused surface damage to

the  protective  optics.  No  damage  was  observed  on  the  rest  of  the  mask  body.  The  goggle

frame  holding  the  optics  did  not  fail  and  was  not  penetrated.  At  V10,  V20  and  V30  speed

setting 170 (see 5.53 above) damage was observed on the optics with all bbs that were able to

hit the target. The goggle frame holding the optics did not fail and was not penetrated.

6.86 The damage observed on the Mask optics was characterised by a visible impact point and

with  extremely  small  stress  lines  in  the  optical  material  radiating  away  from  this  point.  No

mask/optics spalling was observed (see 6.82 above).

6.87  Digicon  0.43g  -  at  V0  the  average  measured  impact  area  caused  by  these  bbs  was

slightly larger than the immediate frontal strike area of the bb itself. The stress lines radiating

away from the impact point were multiple times longer than the diameter of the impact point.

This  result  suggests  that  the  digicon  bb  was  severely  deformed  and  expanded  upon  impact

causing  massive  damage  to  the  optics.  This  was  confirmed  by  examining  the  bb  itself.  The

digicon  was  severely  flattened  and  presented  large  cracks  in  its  structure.  At  V10  the  bb

flattened  and  cracked  upon  impact.  The  damage  and  stress  lines  to  the  mask  optics  was

smaller but still multiple times larger than the diameter of the impact point. At V20 and V30

the  impact  point  and  stress  lines  were  smaller  than  those  recorded  at  V10.  The  bb  was

deformed  but  did  not  crack.  No  spalling  was  observed  at  V10,  V20,  and  V30.  The  Mask

structure itself was dented at V0, V10 but stress marks could not be recorded because this

material is not transparent. At V20 and V30 the goggle frame material did not fail and damage

was very limited.

6.88 Plastic & Bio 0.28g/0.30g - the damage recorder by these bbs was very similar compared

to  that  recorded  in  6.87  above.  Bbs  expanded  and  some  shattered  violently  at  V0.  Impact

points and stress lines were observed though to a smaller degree than those recorded for the

digicon above. Damage assessment confirmed that bbs expanded and deformed upon impact

dramatically increasing stress marks and impact points.

6.89 Plastic & Bio 0.23g/0.25g - the damage recorder by these bbs was very similar compared

to that recorded in 6.85 and 6.86 above. Bbs expanded and some shattered violently at V0.

Impact points and stress lines were observed though to a smaller degree than those recorded

for the heavier bbs above. Damage assessment confirmed that bbs expanded and deformed

upon impact dramatically increasing stress marks and impact points.

6.90 BBBMAX - Damage assessment of the impacts caused by the BBBMAX suggests that this

bb  does  not  expand  or  deform  upon  impact.  None  of  the  bbs  tested  fractured  or  shattered

upon impact and subsequent measurements of the recovered bbs confirmed that they did not

expand or deform. The degree of stress marks and the size of the impact point was smaller in

proportion when compared to all other bbs.

6.91 Plastic & Bio 0.20g - Results of the impacts of these bbs are comparable to the those of

the bbs tested in 6.87 to 6.89 above. At V0 and V10 these bbs expanded and deformed and

some shattered violently. At V20 not all the light bbs were able to hit the target. Those that did

15

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

caused indentations that were smaller than their size or no indentations at all. Tests at V30

were suspended since no bb was able to hit the target.

6.92  Conclusions  -  Plastic,  Bio  and  the  digicon  bbs  expand  and  deform  on  impact  causing

damage  areas  multiple  time  larger  than  their  size.  Impact  points  and  stress  marks  taken

together form massive damage to the optics. The BBBMAX does not expand upon impact and

the impact point and stress marks were measured to be much smaller when compared to other

bbs.

7. Induced expansion

7.1 This test involved setting up a target with a 0.058mm sheet of cardboard against a block

of  ballistic  clay.  A  thinner  block  of  ballistic  clay  was  used  to  allow  the  bbs  to  completely

penetrate it and cause an exit hole on the reverse side.

7.2 The purpose of this test is to document the effects of the expansion and deformation of

the  bbs  caused  by  the  impact  against  a  relatively  hard  cardboard  surface  and  as  they

completely travel through the ballistic clay. By observing the exit hole and the effects of the

impacts  on  the  bbs  themselves  more  accurate  evidence  can  be  recorded  of  the  dynamics

involved.

7.3 The target was placed at V10 and the bbs were fired at the 170 speed setting described in

5.3 above. This test does not simulate any particular real world situation and is only intended

to create a data base of empirical evidence that will be used to confirm the observations and

conclusions in previous tests and from which to make further observations regarding testing on

human targets below.

7.4  By  measuring  the  exit  hole  we  were  able  to  confirm  the  results  of  previous  tests.  The

BBBMAX exit hole  was 6mm wide. This is proof positive  that this bb does not expand upon

impact and is able retain its original form, sphericity and diameter. All the plastic, Bio and the

digicon bbs had measured exit holes that were between 8mm and 10mm wide. This indicates

that these bbs undergo deformation and expansion upon impact with the cardboard and do not

regain their original spherical shape as they pass through the ballistic clay.

7.5  To  further  confirm  this  result  the  same  test  was  carried  out  against  the  ballistic  clay

without the cardboard placed in front. The objective of this second test is to compare the exit

holes of the bbs without the induced expansion and deformation caused by the cardboard. The

resulting  exit  hole  was  the  same  for  the  BBBMAX;  6mm.  The  plastic  bbs  and  the  digicon

formed exit holes that were smaller than those recorder in 7.4 above; in the order of between

6.5 to 8mm.

7.6  By  examining  the  penetration  channels  of  both  tests  7.4  and  7.5  above  to  record  any

further evidence of expansion and deformation, small plastic flakes were discovered along the

inside walls of the channels and at the mouth of exit holes. By subsequently recovering the

fired bbs and examining their surface area it was discovered that the flakes originated from

some of the plastic bbs. This flaking is caused by the violent deceleration of the bbs and their

subsequent  deformation  and  expansion.  A  violent  stoppage  of  the  magnus  effect  from  very

high   rpm   to   near   zero   in   an   extremely   short   period   of   time   and   the   subsequent

deformation/expansion  does  not  afford  all  of  the  plastic  or  bio  material  within  the  bbs

themselves enough time to move from one state to the other in a uniform fashion. This effect

creates a shock wave that travels through the bbs causing surface material to break off. This

result was observed for plastic and bio degradable bbs of Chinese manufacture and not in the

bbs of Japanese manufacture, nor in the digicons, G&G, Bioval or BBBMAX. This empirical data

further supports those outlined in section 4 above.

16

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

7.7 Conclusion - The plastic and bio bbs expand and deform on impact and therefore are able

to transfer more of their energy to the target than the BBBMAX. See section 6.1 to 6.4 above.

Furthermore,  empirical  evidence  confirms  that  most  bbs  are  not  made  with  the  same  high

quality standards and materials than bbs of Japanese manufacture, nor of the digicons, G&G,

Bioval or BBBMAX (FIG I, J).

8. Human Target

This test does not in any way represent a homologation test of the bb ammunition involved.

This test is dangerous and must not be repeated by the reader. This test was conducted under

the supervision of a qualified medical technician in a controlled environment against volunteers

and simulators. We also strongly advise all airsoft players to wear homologated protective full

face gear, gloves with plastic inserts and heavy clothing over the arms and legs.

8.1 Plastic and bio degradable bbs are softer than other harder types of bbs (ex. Some metal

alloy and BBBMAX) and our tests show that they may cause greater damage to human skin

and bone tissue than hard bb projectiles. Most airsoft bb injuries are caused by impacts on

skin tissue in the legs/arms and to the cortical bone tissue in the hands. The degree of these

injuries  depends  upon  the  bb  mass,  velocity  and  the  material  that  it  is  made  of.  The

physiological limitations (in this case, the resistance to impacts) of human skin, subcutaneous

tissue and bone depends strongly on many factors such as for example, age group, skin type

and bone type. There is a great amount of literature on this subject and it has been found that

the impact energy threshold will vary considerably from person to person and from age group

to age group and may be significantly lower for many players. A very good database of high

energy impact injuries has been formed over the years in the sport of paintball. For example,

there have been recorded instances of fractured collar bones caused by impacting paintballs at

low energies. Paintball impact forces are many times more powerful than those of airsoft bb

impacts  and  can  cause  very  serious  injuries.  Due  to  the  very  low  bb  velocities  in  airsoft,

serious  injuries  caused  by  bbs  occur  less  often  and  are  mainly  caused  by  the  negligent

behavior of the players themselves. The main areas of serious bb impact injury are the eyes

and teeth. Other more common impact injuries occur to the skin surface of the face, the hands

and  on  the  legs/arms.  Simple  and  inexpensive  protective  gear  can  be  adopted  to  virtually

eliminate the risk of injuries caused by bb impacts: full face protection (excluding wire mesh

masks), gloves with plastic inserts and thicker clothing.

8.2 - Human Surface and Subcutaneous Tissue (HSST) - Human skin (specific weight of

1.09)  is  considered  very  resistant  to  ballistic  injury  and  has  required  a  lot  of  research  over

many decades to establish a sound database of ballistic evidence. It must be noted that this

study does not deal with penetration of the skin but only with surface injury. Generally, as the

bb projectile begins to impact skin, the retarding force of the skin itself causes it to decelerate

and lose kinetic energy. This rapid deceleration causes the bb to deform as it expands against

the skin surface thus (a) increasing its cross-sectional area towards the impact axis and (b)

transferring more of its kinetic energy into the HSST. Softer bbs will deform more readily and

will  therefore  transfer  more  energy  to  the  HSST  and  over  a  greater/deeper  area  than  will

harder bbs. An impacting bb causes crushing, laceration, stretching and contusion of the tissue

in front and around it. There are many models used to represent the size of the wound, one of

the simplest to understand is expressed as follows:

Ed = Cv*V

Where:

Ed - is dissipated energy

Cv - is a constant depending on the properties of the target material, in this case skin

V - wound size or total inflicted area

17

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

Therefore the size of the inflicted area is directly proportional to the dissipated energy Ed. The

dissipated energy depends upon the time the bb remains in contact with the skin. We know

from the laws of physics that (1) the result of any impact between two objects depends on the

force and time during which the objects are in contact; (2) the time the two impacting objects

remain  in  contact depends on the material properties of  the two objects; (3) the softer the

objects the more time they will remain in contact. Soft bbs impacting on HSST will remain on

the impact zone for a longer period of time therefore dissipating more energy into the HSST

and causing bigger and deeper wounds (FIG K, L).

8.2.1 - Human Bone Tissue (HBT) - Bone has greater density (specific weight of 1.11) and

strength  than  the  surrounding  tissue.  It  is  also  non-elastic.  It  goes  without  saying  that

volunteers for this test were not forthcoming and, therefore, a suitable simulator was sought.

There  are  a  number  of  sources  that  manufacture  simulated  bones used  for  medical  training

applications and ballistic tests. These are manufactured from specially formulated polyurethane

foam forming a cancellous inner core and a harder outer shell simulating cortical bone. During

ballistics  testing  these  products  have  been  shown  to  fracture  in  a  manner  very  similar  to

natural bone providing an excellent reproducible simulation. Simulating a bone impact injury

for the sport of airsoft is very difficult since (a) the bb velocities involved are very low; (b) an

accurate  simulation  requires  that  a  substance  simulating  skin  be  placed  over  the  simulated

bone target area; (c) the most exposed part of the player are the bones is in the hands. To the

best of our knowledge, a suitable substance simulating skin has yet to be found. Therefore,

any test results would need to take this into account. Nevertheless, since it is our opinion that

the great majority of injuries would be restricted to the cortical bone structures in the knuckles

and  fingers  we  can  assume  that  the  amount  of  skin  and  muscle  protecting  these  areas  is

minimal when compared to other areas of the body. In any case, tests show that all bbs will

cause some damage to cortical bone structures and there is ample evidence from the field of

broken teeth caused by bbs of all weight classes and types (though teeth are not considered

bones).  The  observed  difference  in  the  degree  of  injury  will  decrease  as  (a)  the  simulated

target is placed further away from the muzzle of the gas gun; (b) the velocity of the bbs fired

is  lowered;  (c)  a  combination  of  distance  and  speed  thereof.  It  is  beyond  the  scope  of  this

study  to  present  detailed  damage  assessment  since  it  is  not  our  intention  to  mislead  the

reader into believing that some bbs are more or less safe in this regard. Any damage to bones

and teeth is serious and therefore adequate protection must be adopted in order to avoid the

risk of injury. Many low cost solutions are readily available. Nevertheless, our evidence points

to the same conclusions reached in other areas of this study: soft bbs may cause the same if

not  greater damage due to their tendency to deform and expand on impact (FIG M).

8.2.2 Injuries to the muscle mass in the legs and arms are also avoidable but will necessarily

be more common since habitually players will wear a simple BDU over these areas. Again it is

within the scope of this study to present detailed information regarding this specific test but it

is not our intention to mislead the reader into believing that some bbs are more or less safe.

Preventing  injuries  of  this  type  is  easily  achieved  with  the  adoption  of  adequate  protective

equipment.  We  have  chosen,  therefore,  to  present  this  evidence  in  more  detail.  In  the

following  test  the  bbs  were  fired  at  human  volunteer  targets  for  visual  recording  and

measurement  of  surface  injury.  The  distance  between  the  muzzle  of  the  gas  gun  and  the

human target was 5 meters (V5). A survey of the volunteers was taken to decide the location

of impact and the front thigh muscle was elected. The muzzle was aimed at the front thigh

muscle  mass  with  a  BDU  placed  tight  against  the  skin  over  the  impact  zone.  A  medical

technician was called upon to supervise the test and to make periodic visual inspections and

observations of the individual wounds over a period of 4 days.

8.3 A cross section of plastic, bio, hard and heavy bbs was selected and used for this test: a

0.20g, 0.25g, 0.28, BBBMAX and the 0.43g Digicon. The test gun was set at speed rating 130

and 170 (see 5.3 above) and were fired into the target area selected by the volunteers.

18

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

8.4 Two types of damage were noted. The first was in the immediate impact area of the bb

and the second was in the tissue surrounding the impact point.

8.5 Digicon 0.43g - the unlucky volunteer that was struck at V5 with this bb at speed rating

130 and 170 presented massive surface wounding and broken skin. The BDU held tight over

the skin caused the bb to expand and deform permanently at both 130 and 170. At 170 the bb

caused a wound that was 10mm in diameter with an impact area 8mm in diameter. The wound

also caused hardening of tissue in depth and radiating out from the impact area suggesting

sub surface damage. The wound was a uneven combination of broken skin and subcutaneous

hematoma  radiating  out  from  the  impact  point.  At  both  speed  ratings  the  wound  was  still

evident and actually expanded on the second day after the test. Only on day three was the

wound noted to diminish in size. On day 4 the impact zone and the subcutaneous hematoma

were still visible. The volunteer complained of pain even on day four.

8.6 0.28g - Same damage as observed in 8.5 above. At 170 the damage area was larger than

that of  the digicon suggesting much more expansion of the bb due to the faster speed and

force of impact. On day 4 the observations were the same as in 8.5 above.

8.7 0.25g - Due to the faster speed of the bb and therefore of the impact force the wound

caused by the impact of this bb was larger than that of the Digicon and that of the 0.28g bb.

The wound can be described in the same terms as in 8.5 above and diminished in size only on

day 3 and 4.

8.8  BBBMAX  -  The wound caused  by  the  BBBMAX fired  at  170 was  fundamentally  different

from that of the other bbs tested. Immediately no impact point was identified suggesting that

it was very small. The total measured size of the wound was 13mm in diameter and can be

described as a subcutaneous hematoma. After only 5 hours the wound changed dramatically

as the hematoma began to be absorbed and a small impact point 3mm in diameter became

apparent. After 24 hours the impact point completely disappeared and only slight bruising was

apparent.  Day  4  the  size  of  the  wound  was  smaller  with  obvious  signs  of  healing.  This

difference  can  be  attributed  to  the  fact  that  the  BBBMAX  does  not  expand  on  impact  and

therefore is unable to transfer energy to the target as efficiently as the other bbs tested. This

also explains the very focused and small impact point identified after 5 hours from impact.

8.9 0.20g - The most interesting results were observed from the impact of the 0.20g bb fired

at  the  same  volunteer  that  was  struck  with  the  BBBMAX  (opposite  leg).  This  wound  was  a

massive 15mm in diameter with a very large impact point measuring 7mm in diameter. The

image taken immediately after impact shows a barely visible subcutaneous hematoma around

the lower part of the open wound suggesting a very deep injury. On day 4 the wound was still

10mm in  diameter with  an  impact  point  4mm in  diameter.  This compelling evidence further

supports  the  results  from  previous  tests:  plastic  and  bio  plastic  bbs  expand  and  deform  on

impact causing damage that is in proportion much larger than their diameter and much larger

than their immediate frontal impact areas.

8.10 Conclusion: Impacts on human skin and subcutaneous tissue. The evidence shows that

the BBBMAX causes less damage to human targets since the structure of the bb itself does not

allow for an efficient transfer of energy upon impact. This test leads us to believe that plastic

and bio bbs can potentially cause more damage to skin tissue than harder bbs. Moreover, our

evidence allows us to conclude that the softer the bb the more damage it causes to skin tissue.

9. Conclusions

The  aim  of  this  study  was  to  determine  the  performance  and  safety  of  the  bb  ammunition

tested.  We  believe  that  the  tested  number,  weight,  brand  and  country  of  manufacture

represents an accurate cross-section of the market in general.

19

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

9.1  The  empirical  evidence  accumulated  allows  us  to  conclude  that  all  the  tested  bb

ammunition is safe for use in the sport/game of airsoft. We suggest the use of certified full

face and hand protection (in the form of gloves with plastic inserts) and minimum engagement

distances to be adopted.

9.2 Bbs in general can be divided into 2 very broad categories:

SOFT - Bbs made of plastic, of bio degradable materials, and of some low grade metal

alloys are defined as soft and will cause more damage (on human skin and materials)

when  compared  to  hard  bbs.  We  stress  this point  throughout  this  study  since  it  is  a

commonly  overlooked  factor  when  assessing  damage  and  the  potential  for  damage.

This  is  due  to  the  elastic  properties  of  the  materials  used  to  make  these  bbs.  Upon

impact these bbs will deform and expand causing the bb to (a) remain in contact with

the impact area for a much longer period of time than harder bbs; (b) produce damage

on a much larger area in the impact zone. Soft bbs transfer energy more efficiently to

the impact area when compared to the harder bbs.

HARD - Bbs such as the BBBMAX are defined as hard. These bbs will not deform on

impact. This characteristic drastically reduces the time they remain in contact with the

impact point relative to their softer competitors described in 9.2 above. This means that

a  lower  amount  of  energy  is  transferred  from  the  bb  to  the  impact  area.  A  large

proportion of the energy is dissipated by the bb as it rebounds off the impacted area.

9.4 Good ballistic performance depends entirely on consistent density and consistent sphericity

within a bb, from bb to bb and within the same lot of a particular manufacturer. In this regard,

the BBBMAX markedly stands out from the rest of the bbs tested and represents as near an

ideal spherical projectile as we have ever tested. The material used to manufacture BBBMAX

obviously allows this projectile to better cope with the forces it is interacting with both in the

barrel of the gun and as it travels along its intended trajectory. Of the more traditional bbs,

those  of  Japanese  manufacture,  the  bioval  bio  bbs  and  the  digicons  outperformed  their

competitors by a wide margin.

20

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

ANNEX

21

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

22

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

23

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

24

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

25

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

26

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

27

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

28

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

29

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

30

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

31

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

32

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

33

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

34

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

35

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

36

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

37

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

38

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

39

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

40

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

41

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

42

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

43

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

44

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

45

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

46

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

47

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

48

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

49

Levante Labs

Std. Fd.U.W.

1 Centro Carvina

6807 Taverne

Switzerland

Test b908

50